Appendix

Aluminum Futures Contract Specifications

(Revised)

| Product | Aluminum |
| --- | --- |
| Contract Size | 5 metric tons/lot |
| Price Quotation | Yuan (RMB)/metric ton |
| Minimum Price Fluctuation | 5 Yuan/metric ton |
| Daily Price Limit | Within ±3% of the settlement price of the preceding trading day |
| Listed Contracts | Monthly contract for the most recent 12 months |
| Trading Hours | 9:00 a.m. to 11:30 a.m., 1:30 p.m. to 3:00 p.m., and other hours specified by the Exchange (Beijing Time) |
| Last Trading Day | 15th day of the contract month (postponed accordingly if it is a legal holiday in China and subject to separate adjustment and announcement by the Exchange if it falls in the Spring Festival month or any other month specially designated by the Exchange) |
| Delivery Period | Three consecutive business days after the last trading day |
| Grade and Quality Specifications | Standard products: AL99.70 aluminum ingots as prescribed in National Standard GB/T 1196-2017, with aluminum content not less than 99.70%. Substitutions: 1. AL99.80 and AL99.85 aluminum ingots as prescribed in National Standard GB/T 1196-2017. 2. P1020A aluminum ingots. |
| Delivery Venue | Delivery warehouses designated by the Exchange |
| Minimum Trade Margin | 5% of the contract value |
| Settlement Type | Physical delivery |
| Delivery Unit | 25 metric tons |
| Contract Symbol | AL |
| Listing Exchange | Shanghai Futures Exchange |

Appendix to Aluminum Futures Contract Specifications

I.	Delivery Unit

The contract size for aluminum futures is 5 metric tons per lot; the delivery unit is 25 metric tons per warrant. Delivery shall be made in whole warrants.

II.	Quality Standards

(1)	The aluminum content, impurity level, and other properties of aluminum used for physical delivery shall conform to the specifications of National Standard GB/T 1196-2017 for AL99.70.

(2)	Shape and weight: Deliverable aluminum shall be in the form of ingots. Each ingot of domestic aluminum shall weigh 15 kg ± 2 kg, 20 kg ± 2 kg, or 25 kg ± 2 kg; each ingot of imported aluminum shall weigh between 12 kg and 26 kg.

(3)	For each warrant, the tolerance shall not exceed ±2% and the pound difference shall not exceed ±0.1%.

(4)	Aluminum underlying each warrant shall consist of commodity of the same manufacturer, grade (designation), registered trademark, quality grade, shape, and packaged quantity (secured into bundles of similar weight).

(5)	Aluminum underlying each warrant shall be of a registered brand approved by SHFE, accompanied by corresponding certificate of quality.

(6)	Warrant shall be issued by a Designated Delivery Warehouse only after its inspection and acceptance of the commodity according to applicable rules.

III.	Manufacturers and Registered Brands Recognized by SHFE

Aluminum used for physical delivery shall be of a brand registered with SHFE. The registered brands and the standards of premiums and discounts will be separately specified and announced by SHFE.

IV.	Designated Delivery Warehouses

Designated Delivery Warehouses and the standards of premiums and discounts applied to delivery warehouses at different locations will be separately specified and announced by SHFE.